## Slide 1: Report on Electrical Characterisation of thin film transistors based on TMTES-PS organic semiconductor as prospective X-ray detectors
The transistors were fabricated by the University of Barcelona. The electrical characterization was performed by Mikhail Bandurist in collaboration with Professor Laura Basiricò and Ilaria Fratelli at the University of Bologna.

## Slide 2: General features
Batch made up of 4 different material compositions
Every composition is used in 2 substrates, each one with 4 OFET with common gate
32 transistors in total, 8 for every composition
TMTES:PS as active material, with fixed 2:1 ratio
Channel features: L=25µm, W=2500µm, C=17.3·F/

## Slide 3: Sample structure
The batch consists of thin film transistors with Au electrodes, SiO2 insulator layer and the active channel as the blended mixture of TMTES and PS.
The batch includes 4 sets with different TMTES:PS ratio: (17:3), (9:1), (19:1) and (39:1).
Each set includes 2 samples (substrates), each one with 4 devices (transistors) with common gate.
32 devices in total, 8 for each TMTES:PS ratio.

## Slide 4: Table (Ratios 17:3 and 9:1)
TMTES:PS | Sample_device | ON/OFF (#*10^3) | SS (V/ec) | Vth (V) | mu (cm^2/(V*s))
17:3 | S5_d00 | 190.25 | 0.971±0.016 | 1.20±0.04 | 0.98±0.02
 | S5_d01 | 28.23 | 0.70±0.03 | 1.18±0.04 | 0.955±0.05
 | S5_d10 | 2.27 | 1.14±0.02 | 1.77±0.03 | 0.092±0.016
 | S5_d11 | No data | No data | No data | No data
 | S6_d00 | 116.34 | 0.526±0.006 | 1.41±0.04 | 0.798±0.02
 | S6_d01 | 1.53 | 0.709±0.010 | 1.51±0.04 | 0.762±0.02
 | S6_d10 | 272.19 | 0.62±0.02 | 1.73±0.04 | 0.755±0.06
 | S6_d11 | 51.32 | 0.63±0.03 | 1.91±0.10 | 0.80±0.08
9:1 | S11_d00 | 20.31 | 0.961±0.013 | 2.49±0.04 | 0.547±0.014
 | S11_d01 | 3.77 | 0.71±0.02 | 1.87±0.03 | 0.519±0.04
 | S11_d10 | 1.95 | 1.214±0.009 | 2.72±0.05 | 0.0549±0.006
 | S11_d11 | 0.40 | 0.985±0.015 | 7.63±0.8 | 0.020±0.015
 | S12_d00 | 58.68 | 0.638±0.002 | 1.76±0.03 | 0.650±0.005
 | S12_d01 | 1.02 | 1.379±0.017 | 1.66±0.04 | 0.0185±0.009
 | S12_d10 | 16.14 | 0.582±0.005 | 1.69±0.04 | 0.727±0.014
 | S12_d11 | 12.07 | 0.571±0.007 | 1.91±0.04 | 0.707±0.02
Common features: • W = 2500 um • Thickness of SiO2 insulator layer = 200 nm • No encapsulation
• L = 25 um • Capacitance per unit area Ci = 17.3 nF/cm^2
• Pixel area = 0.00425 cm^2

## Slide 5: Table (Ratios 19:1 and 39:1)
TMTES:PS | Sample_device | ON/OFF (#*10^3) | SS (V/ec) | Vth (V) | mu (cm^2/(V*s))
19:1 | S17_d00 | 22.32 | 2.05±0.06 | 5.83±0.11 | 0.331±0.014
 | S17_d01 | 22.10 | 2.03±0.05 | 5.27±0.12 | 0.388±0.013
 | S17_d10 | 9.42 | 2.441±0.006 | 5.88±0.09 | 0.376±0.001
 | S17_d11 | 10.39 | 2.49±0.080 | 6.01±0.12 | 0.340±0.012
 | S18_d00 | 98.24 | 1.32±0.05 | 5.62±0.11 | 0.456±0.03
 | S18_d01 | 51.79 | 1.56±0.05 | 5.50±0.11 | 0.471±0.02
 | S18_d10 | 44.13 | 2.00±0.07 | 6.16±0.12 | 0.412±0.017
 | S18_d11 | No data | No data | No data | No data
39:1 | S23_d00 | 4.71 | 3.19±0.02 | 8.43±0.14 | 0.315±0.002
 | S23_d01 | 22.17 | 3.39±0.04 | 8.95±0.15 | 0.305±0.003
 | S23_d10 | 24.44 | 2.525±0.019 | 8.57±0.09 | 0.279±0.003
 | S23_d11 | 24.25 | 3.05±0.05 | 8.55±0.13 | 0.286±0.005
 | S24_d00 | 6.65 | 3.22±0.03 | 11.82±0.11 | 0.230±0.003
 | S24_d01 | 0.29 | 3.76±0.06 | 14.12±0.17 | 0.000180±0.004
 | S24_d10 | 11.98 | 4.76±0.05 | 16.40±0.09 | 0.1609±0.002
 | S24_d11 | 7.65 | 3.69±0.04 | 12.82±0.10 | 0.195±0.003
Common features: • W = 2500 um • Thickness of SiO2 insulator layer = 200 nm • No encapsulation
• L = 25 um • Capacitance per unit area Ci = 17.3 nF/cm^2
• Pixel area = 0.00425 cm^2

## Slide 6: Ratio 17:3
Sample5_device00
Sample5_device01
Sample5_device10
Sample5_device11 (no data)
Sample6_device00
Sample6_device01
Sample6_device10
Sample6_device11

## Slide 7: Sample5_device00
ON/OFF = 190.25 * 103
SS = 0.971±0.016 V/dec
Vth = 1.20±0.04 V
mu = 0.98±0.02 cm2/(V*s)

## Slide 8: Sample5_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 9: Sample5_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 10: Sample6_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 11: Sample6_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 12: Sample6_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 13: Sample6_device11
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 14: Ratio 9:1
Sample11_device00
Sample11_device01
Sample11_device10
Sample11_device11
Sample12_device00
Sample12_device01
Sample12_device10
Sample12_device11

## Slide 15: Sample11_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 16: Sample11_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 17: Sample11_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 18: Sample11_device11
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 19: Sample12_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 20: Sample12_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 21: Sample12_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 22: Sample12_device11
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 23: Ratio 19:1
Sample17_device00
Sample17_device01
Sample17_device10
Sample17_device11
Sample18_device00
Sample18_device01
Sample18_device10
Sample18_device11 (no data)

## Slide 24: Sample17_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 25: Sample17_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 26: Sample17_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 27: Sample17_device11
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 28: Sample18_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 29: Sample18_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 30: Sample18_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 31: Ratio 39:1
Sample23_device00
Sample23_device01
Sample23_device10
Sample23_device11
Sample24_device00
Sample24_device01
Sample24_device10
Sample624_device11

## Slide 32: Sample23_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 33: Sample23_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 34: Sample23_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 35: Sample23_device11
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 36: Sample24_device00
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 37: Sample24_device01
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 38: Sample24_device10
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)

## Slide 39: Sample24_device11
ON/OFF = x * 103
SS = x V/dec
Vth = x V
mu = x cm2/(V*s)