## Slide 1: Report 12/11/2023
Electrical characterization on samples from Batch 2

## Slide 3: Sample 1
Sample1_device1 th=4.5±0.5 nm
Sample1_device2 th=5.4±0.7 nm
Sample1_device3 th=6.0±0.6 nm
Sample1_device4 th=2.6±0.3 nm
Sample1_device5 th=2.9±0.7 nm

## Slide 4: Sample1_device1

## Slide 5: Sample1_device1

## Slide 6: Sample1_device2

## Slide 7: Sample1_device2

## Slide 8: Sample1_device3

## Slide 9: Sample1_device3

## Slide 10: Sample1_device4

## Slide 11: Sample1_device4

## Slide 12: Sample1_device5

## Slide 13: Sample1_device5

## Slide 14: Sample 4
Sample4_device1 th=2.4±0.3 nm

## Slide 15: Sample4_device1

## Slide 16: Sample4_device1

## Slide 17: Sample 5
Sample5_device1 th=8.9±0.9 nm
Sample5_device2 th=5.8±0.9 nm
Sample5_device3 th=2.8±0.4 nm
Sample5_device4 th=3.1±0.5 nm

## Slide 18: Sample5_device1

## Slide 19: Sample5_device1

## Slide 20: Sample5_device2

## Slide 21: Sample5_device2

## Slide 22: Sample5_device3

## Slide 23: Sample5_device4

## Slide 24: Sample5_device4

## Slide 25: Sample 6
Sample6_device1 th=8.3±0.9 nm
Sample6_device3 th=10.8±0.6 nm
Sample6_device5 th=6.3±0.6 nm

## Slide 26: Sample6_device1

## Slide 27: Sample6_device1

## Slide 28: Sample6_device3

## Slide 29: Sample6_device3

## Slide 30: Sample6_device5

## Slide 31: Sample6_device5

## Slide 32: Sample 7
Sample7_device1 th=2.8±0.4 nm
Sample7_device4 th=3.8±0.4 nm
Sample7_device5 th=5.7±0.3 nm

## Slide 33: Sample7_device1

## Slide 34: Sample7_device1

## Slide 35: Sample7_device4

## Slide 36: Sample7_device4

## Slide 37: Sample7_device5

## Slide 38: Sample7_device5

## Slide 39: Sample 8
Sample8_device1 th=6.2±0.6 nm

## Slide 40: Sample8_device1

## Slide 41: Sample8_device1

## Slide 42: Sample 9
Sample9_device2 th=7.8±0.7 nm
Sample9_device3 th=10.8±1.4 nm

## Slide 43: Sample9_device2

## Slide 44: Sample9_device2

## Slide 45: Sample9_device3

## Slide 46: Sample9_device3

## Slide 47: Sample 10
Sample10_device1 th=3.9±0.5 nm
Sample10_device2 th=2.6±0.3 nm
Sample10_device3 th=8.7±0.4 nm
Sample10_device5 th=8.0±0.5 nm
Sample10_device6 th=9.4±0.5 nm

## Slide 48: Sample10_device1

## Slide 49: Sample10_device1

## Slide 50: Sample10_device2

## Slide 51: Sample10_device2

## Slide 52: Sample10_device3

## Slide 53: Sample10_device3

## Slide 54: Sample10_device5

## Slide 55: Sample10_device5

## Slide 56: Sample10_device6

## Slide 57: Sample10_device6

## Slide 58: Sample 11
Sample11_device1 th=3.6±0.4 nm
Sample11_device3 th=9.2±0.8 nm

## Slide 59: Sample11_device1

## Slide 60: Sample11_device1

## Slide 61: Sample11_device3

## Slide 62: Sample11_device3

## Slide 63: Sample 12
Sample12_device1 th=4.8±0.6 nm
Sample12_device2 th=2.4±0.3 nm
Sample12_device3 th=3.3±0.3 nm
Sample12_device4 th=4.8±0.3 nm

## Slide 64: Sample12_device1

## Slide 65: Sample12_device1

## Slide 66: Sample12_device2

## Slide 67: Sample12_device2

## Slide 68: Sample12_device3

## Slide 69: Sample12_device3

## Slide 70: Sample12_device4

## Slide 71: Sample12_device4

## Slide 72: Sample 14
Sample14_device1 th=4.8±0.6 nm
Sample14_device2 th=2.4±0.3 nm
Sample14_device3 th=3.3±0.3 nm
Sample14_device4 th=4.8±0.3 nm

## Slide 73: Sample14_device1

## Slide 74: Sample14_device1

## Slide 75: Sample14_device2

## Slide 76: Sample14_device2

## Slide 77: Sample14_device3

## Slide 78: Sample14_device3

## Slide 79: Sample14_device4

## Slide 80: Sample14_device4