## Slide 1: Report on Electrical Characterisation of 1-layer MoS2 thin film transistors as prospective X-ray detectors
The transistors were fabricated by Adrian Tamayo at the University of Strasbourg. The electrical characterization was performed by Mikhail Bandurist in collaboration with Ilaria Fratelli and professor Laura Basiricò at the University of Bologna.

## Slide 2: Samples structure and characterization
MEASUREMENTS
n-type semiconductor
Low stability in aire, storage in glove box
Electrical measurements were performed reaching VDS = 1 V, and VGS = -60 to 60 V
Delay 100 ms and ΔVGS = 0.5 V
Top contact / Bottom gate
Note: If you need, you can scratch the surface of the substrates to access the gate.
Au/Cr 45/3 nm
MoS2
BCB layer 50 nm
SiOx 278 nm
Si

## Slide 3: Table (Samples 1-8)
Sample_device | W (um) | L (um) | MoS2 thick (nm) | ON/OFF (#/10^6) | SS (V/dec) | Vth (V) | mu (cm^2/(V*s))
S1_d1 | 19.8 | 2.6 | 4.5±0.5 | 0.22 | 4.32±0.16 | -8.75±0.11 | 0.2156±0.0013
S1_d2 | 11.6 | 2.3 | 5.4±0.7 | 0.04 | 12.67±0.08 | 6.87±0.13 | 0.01684±0.00010
S1_d3 | 21.2 | 2.7 | 6.0±0.6 | 3.23 | 2.71±0.05 | -32.1±-.7 | 0.0049±0.0002
S1_d4 | 17.6 | 2.3 | 2.6±0.3 | 0.01 | 8.70±0.12 | 4.6±0.3 | 0.01091±0.00002
S1_d5 | 14.1 | 2.7 | 2.9±0.7 | No current | No current | No current | No current
S4_d1 | 13.6 | 2.3 | 2.4±0.3 | 11.30 | 2.85±0.04 | -43.0±0.6 | 0.478±0.012
S5_d1 | 21.8 | 2.3 | 8.9±0.9 | No current | No current | No current | No current
S5_d2 | 20.9 | 2.2 | 5.8±0.9 | 0.04 | 5.085±0.26 | -4.62±0.08 | 0.01113±0.00006
S5_d3 | 16.4 | 2 | 2.8±0.4 | No current | No current | No current | No current
S5_d4 | No data | No data | 3.1±0.5 | No current | No current | No current | No current
S6_d1 | 24.5 | 2.3 | 8.3±0.9 | 14.20 | 4.98±00.10 | -15.61±0.07 | 0.96±0.007
S6_d2 | 21.1 | 2.1 | 10.8±0.6 | No current | No current | No current | No current
S6_d3 | 14.7 | 2.1 | 6.3±0.6 | 20.70 | 4.66±0.10 | -6.30±0.10 | 0.26280±0.0014
S7_d1 | 10 | 1.9 | 2.8±0.4 | 3.18 | 5.92±0.07 | -3.2±0.2 | 0.0483±0.0005
S7_d4 | 13.8 | 2.2 | 3.8±0.4 | 0.00 | 6.5±0.3 | -9.23±0.08 | 0.00919±0.00004
S7_d5 | 32.1 | 1.3 | 5.7±0.3 | No current | No current | No current | No current
S8_d1 | 8.2 | 2 | 6.2±0.6 | 0.02 | 9.57±0.12 | 10.76±0.16 | 0.2443±0.0016
Common features: • Batch 2 • No encapsulation • Thickness of SiO2 insulator layer = 278 nm
• Capacitance per unit area Ci = 0.0124 (uF/cm^2)

## Slide 4: Table (Samples 9-14)
Sample_device | W (um) | L (um) | MoS2 thick (nm) | ON/OFF (#/10^6) | SS (V/dec) | Vth (V) | mu (cm^2/(V*s))
S9_d2 | 20.6 | 2.4 | 7.8±0.7 | Not reliable | 4.03±0.03 | Not reliable | 0.028581272
S9_d3 | 39.6 | 2.2 | 10.8±1.4 | 0.82 | 4.19±0.05 | -14.14±0.09 | 0.784±0.006
S10_d1 | 12.4 | 3 | 3.9±0.5 | No contact between the sample and the tips | No contact between the sample and the tips | No contact between the sample and the tips | No contact between the sample and the tips
S10_d2 | 16.6 | 2.6 | 2.6±0.3 | 0.50 | 10.2±1.0 | 22.3±0.8 | 0.0197±0.0006
S10_d3 | 27.8 | 3.3 | 8.7±0.4 | 0.21 | 2.54±0.05 | -28.37±0.08 | 0.713±0.004
S10_d5 | 14.4 | 3.2 | 8.0±0.5 | No current | No current | No current | No current
S10_d6 | 14.8 | 4.4 | 9.4±0.5 | 0.01 | 8.50±0.17 | -45.0±0.4 | 0.329±0.005
S11_d1 | 14.8 | 3.3 | 3.6±0.4 | 0.00 | 13.9±0.10 | 20.2±0.7 | 0.0309±0.0008
S11_d3 | 8.6 | 2.9 | 9.2±0.8 | 6.44 | 3.66±0.07 | -25.02±0.9 | 0.3481±0.0017
S12_d1 | 9.9 | 2.9 | 4.8±0.6 | No current | No current | No current | No current
S12_d2 | 13.2 | 3.1 | 2.4±0.3 | 0.07 | 6.50±0.09 | 5.1±0.3 | 0.1231±0.0019
S12_d3 | 20 | 3.8 | 3.3±03 | 0.00 | 8.62±0.11 | -8.11±0.09 | 0.0677±0.0004
S12_d4 | 18.5 | 3.1 | 4.8±0.3 | 1.08 | 6.411±0.004 | -10.20±0.10 | 0.0331±0.0003
S14_d1 | 20.1 | 3.5 | 4.8±0.6 | 9.18 | 4.18±0.11 | -10.31±0.10 | 0.353±0.003
S14_d2 | 15.5 | 3.2 | 2.4±0.3 | 15.80 | 2.83±0.03 | -42.1±0.5 | 0.288±0.006
S14_d3 | 21.1 | 3.7 | 3.3±0.3 | 12.10 | 3.58±0.03 | -13.22±0.05 | 0.1267±0.0003
S14_d4 | 16.4 | 3.2 | 4.8±0.3 | 15.70 | 2.67±0.03 | -55.3±0.7 | 0.274±0.007
Average ± StdDev |  |  |  | 5±7 | 6±3 | -13±20 | 0.2±0.3
Common features: • Batch 2 • No encapsulation • Thickness of SiO2 insulator layer = 278 nm
• Capacitance per unit area Ci = 0.0124 (uF/cm^2)

## Slide 5: Sample 1
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1
Device 2
Device 3
Device 4
Device 5

## Slide 6: Sample1_device1
ON/OFF = 0.22*106
SS = 4.32 ± 0.16 V/dec
Vth = -8.75 ± 0.11 V
mu = 0.2156 ± 0.0013 cm2/(V*s)
trfSat and trfLin are fine, hysteresis is present, but small, however, the output curves show no field effect.
Device 1

## Slide 7: Sample1_device2
ON/OFF = 0.04 * 106
SS = 12.67 ± 0.08 V/dec
Vth = 6.87 ± 0.13 V
mu = 0.01684 ± 0.00010 cm2/(V*s)
At trfSat and trfLin a hysteresis is present, the output curves show no field effect.
Device 2

## Slide 8: Sample1_device3
ON/OFF = 3.23*106
SS = 2.71 ± 0.05 V/dec
Vth = -32.1 ± 0.7 V
mu = 0.0049±0.0002 cm2/(V*s)
Device 3

## Slide 9: Sample1_device4
ON/OFF = 0.01*106
SS = 8.70±0.12 V/dec
Vth = 4.6±0.3 V
mu = 0.01091±0.00002 cm2/(V*s)
At trfSat and trfLin a hysteresis is significant, however the output curves show good field effect.
Device 4

## Slide 10: Sample1_device5
ON/OFF = -
SS = -
Vth = -
mu = -
No signal is observed, possibly, bad connection was present.
Device 5

## Slide 11: Sample 4
Device 1
Device 2
Device 3
Device 4
Device 1
Device 2
Device 3
Device 4

## Slide 12: Sample4_device1
ON/OFF = 11.30*106
SS = 2.85±0.04 V/dec
Vth = -43.0±0.6 V
mu = 0.478±0.012 cm2/(V*s)
trfSat is comparable to the one sent by Adrian, output curves show no field effect.

## Slide 13: Sample 5
Device 1
Device 2
Device 3
Device 4
Device 1
Device 3
Device 2
Device 4

## Slide 14: Sample5_device1
ON/OFF = -
SS = -
Vth = -
mu = -
No signal is observed, probably, bad connection.
Device 1

## Slide 15: Sample5_device2
ON/OFF = 0.04 *106
SS = 5.085±0.26 V/dec
Vth = -4.62±0.08 V
mu = 0.01113±0.00006 cm2/(V*s)
At trfSat and trfLin significant hysteresis is observed, the output curves show no field effect.
Device 2

## Slide 16: Sample5_device3
ON/OFF = -
SS = -
Vth = -
mu = -
No signal is observed (Idrain is almost zero), probably, bad connection.
Device 3

## Slide 17: Sample5_device4
ON/OFF = -
SS = -
Vth = -
mu = -
No signal is observed.
Device 4

## Slide 18: Sample 6
Device 2
Device 3
Device 4
Device 5
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 19: Sample6_device1
ON/OFF = 14.20*106
SS = 4.98±00.10 V/dec
Vth = -15.61±0.07 V
mu = 0.96±0.007 cm2/(V*s)
trfSat and trfLin are fine, small hysteresis is present, the output curves show field effect at VGate below 30V.
Device 1

## Slide 20: Sample6_device3
ON/OFF = -
SS = -
Vth = -
mu = -
No signal was observed, probably, bad connection.
Device 3

## Slide 21: Sample6_device5
ON/OFF = 20.7*106
SS = 4.66±0.10 V/dec
Vth = -6.30±0.10 V
mu = 0.2628±0.0014 cm2/(V*s)
At trfSat and trfLin hysteresis is present, output curves show good field effect.
Device 5

## Slide 22: Sample 7
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 23: Sample7_device1
ON/OFF = 3.18*106
SS = 5.92±0.07 V/dec
Vth = -3.2±0.2 V
mu = 0.0483±0.0005 cm2/(V*s)
At trfSat and trfLin significant hysteresis is observed, the output curves show good field effect.
Device 1

## Slide 24: Sample7_device4
ON/OFF = 0.00398*106
SS = 6.5±0.3 V/dec
Vth = -9.23±0.08 V
mu = 0.00919±0.00004 cm2/(V*s)
At trfSat and trfLin significant hysteresis is observed, the output curves show absolutely no field effect.
Device 4

## Slide 25: Sample7_device5
ON/OFF = -
SS = -
Vth = -
mu = -
No signal at trfSat is observed, at VGate=10V IDrain is about 10-10 A. The output curves show ohmic behaviour, which implies independence of the IDrain on VGate (ignorance of the gate from the active channel).
Device 5

## Slide 26: Sample 8
Device 1
Device 2
Device 3
Device 4
Device 5
Device 6
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 27: Sample8_device1
ON/OFF = 0.02*106
SS = 9.57±0.12 V/dec
Vth = 10.76±0.16 V
mu = 0.2443±0.0016 cm2/(V*s)
At trfSat and trfLin hysteresis is observed, the output curves show good field effect.
Device 1

## Slide 28: Sample 9
Device 1
Device 2
Device 3
Device 1
Device 2
Device 3

## Slide 29: Sample9_device2
ON/OFF = -
SS = -
Vth = -
mu = -
trfSat curve behaves well only below 0-10V (compliance?), trfLin performs well even with hysteresis, the output curves show good field effect. The measured properties are considered unreliable.
Device 2

## Slide 30: Sample9_device3
ON/OFF = 0.82*106
SS = 4.19±0.05 V/dec
Vth = -14.14±0.09 V
mu = 0.784±0.006 cm2/(V*s)
At trfSat and trfLin hysteresis is observed, the output curves show field effect at VGate <= 30V.
Device 3

## Slide 31: Sample 10
Device 2
Device 3
Device 4
Device 5
Device 6
Device 1
Device 3
Device 2
Device 4
Device 5
Device 6

## Slide 32: Sample10_device1
ON/OFF = -
SS = -
Vth = -
mu = -
trfSat is not finished because of constant interruption from the interlock, so I used the trfSat curve that got the longest measurement range. After that the connection between the sample and the tips was completely lost.
Device 1

## Slide 33: Sample10_device2
ON/OFF = 0.50*106
SS = 10.2±1.0 V/dec
Vth = 22.3±0.8 V
mu = 0.0197±0.0006 cm2/(V*s)
At trfSat and trfLin significant hysteresis is present, however, the output curves show good field effect.
Device 2

## Slide 34: Sample10_device3
ON/OFF = 0.21*106
SS = 2.54±0.05 V/dec
Vth = -28.37±0.08 V
mu = 0.713±0.004 cm2/(V*s)
trfSat and trfLin perform well with small hysteresis, the output curves show field effect at VGate below 30V.
Device 3

## Slide 35: Sample10_device5
ON/OFF = -
SS = -
Vth = -
mu = -
No signal is observed, probably, bad connection.
Device 5

## Slide 36: Sample10_device6
ON/OFF = 0.01*106
SS = 8.50±0.17 V/dec
Vth = -45.0±0.4 V
mu = 0.329±0.005 cm2/(V*s)
trfSat and trfLin perform well with small hysteresis, the output curves show field effect only at VGate below -10V.
Device 6

## Slide 37: Sample 11
Device 1
Device 2
Device 3
Device 4
Device 5
Device 2
Device 4
Device 1
Device 3
Device 5

## Slide 38: Sample11_device1
ON/OFF = 0.000643*106
SS = 13.9±0.10 V/dec
Vth = 20.2±0.7 V
mu = 0.0309±0.0008 cm2/(V*s)
trfSat and trfLin have significant hysteresis, however, the output curves show good field effect.
Device 1

## Slide 39: Sample11_device3
ON/OFF = 6.44*106
SS = 3.66±0.07 V/dec
Vth = -25.02±0.9 V
mu = 0.3481±0.0017 cm2/(V*s)
trfSat and trfLin perform well with small hysteresis, the output curves show field effect only at VGate below 30V.
Device 3

## Slide 40: Sample 12
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 41: Sample12_device1
ON/OFF = -
SS = -
Vth = -
mu = -
No signal is observed, probably, bad connection.
Device 1

## Slide 42: Sample12_device2
ON/OFF = 0.07*106
SS = 6.50±0.09 V/dec
Vth = 5.1±0.3 V
mu = 0.1231±0.0019 cm2/(V*s)
trfSat and trfLin have significant hysteresis, however, the output curves show good field effect.
Device 2

## Slide 43: Sample12_device3
ON/OFF = 0.00326*106
SS = 8.62±0.11 V/dec
Vth = -8.11±0.09 V
mu = 0.0677±0.0004 cm2/(V*s)
trfSat and trfLin have significant hysteresis, however, the output curves show absolutely no field effect.
Device 3

## Slide 44: Sample12_device4
ON/OFF = 1.08*106
SS = 6.411±0.004 V/dec
Vth = -10.20±0.10 V
mu = 0.0331±0.0003 cm2/(V*s)
trfSat and trfLin have medium hysteresis, the output curves show field effect only at VGate below 10V.
Device 4

## Slide 45: Sample 14
Device 1
Device 2
Device 3
Device 4
Device 2
Device 4
Device 1
Device 3

## Slide 46: Sample14_device1
ON/OFF = 9.18*106
SS = 4.18±0.11 V/dec
Vth = -10.31±0.10 V
mu = 0.353±0.003 cm2/(V*s)
trfSat and trfLin perform well even with hysteresis, the output curves show field effect at VGate below 30V.
Device 1

## Slide 47: Sample14_device2
ON/OFF = 15.80*106
SS = 2.83±0.03 V/dec
Vth = -42.1±0.5 V
mu = 0.288±0.006 cm2/(V*s)
trfSat and trfLin perform well, however, the output curves are completely linear.
Device 2

## Slide 48: Sample14_device3
ON/OFF = 12.10*106
SS = 3.58±0.03 V/dec
Vth = -13.22±0.05 V
mu = 0.1267±0.0003 cm2/(V*s)
trfSat and trfLin have siginificant hysteresis, the output curves show field effect only at VGate below 10V.
Device 3

## Slide 49: Sample14_device4
ON/OFF = 15.70*106
SS = 2.67±0.03 V/dec
Vth = -55.3±0.7 V
mu = 0.274±0.007 cm2/(V*s)
trfSat and trfLin perfrom well, howeverm the output curves show absolutely no field effect.
Device 4

## Slide 50: Comparison with the data from literature:
Ji Heon Kim, Tae Ho Kim, Hyunjea Lee, Young Ran Park, Woong Choi, Cheol Jin Lee; Thickness-dependent electron mobility of single and few-layer MoS2 thin-film transistors. AIP Advances 1 June 2016; 6 (6): 065106. https://doi.org/10.1063/1.4953809
Schematic cross-section of a MoS2 thin-film transistor fabricated in this study.
(b) Optical micrograph of a representative MoS2 transistor.
Bottom gate, Top contact
SiO2 dielectric
Au electrodes
For 1L TFT:
Channel width W ∝ 10 um
Channel length L ∝ 5 um
Main parameters for 1L TFT:
ON/OFF ∝ 107
mu ∝ 10 cm2/(V*s)
SS ∝ 60mV/decade
Deposition method – mechanical exfoliation

## Slide 51: Comparison with the data from literature:
2) Single-layer MoS2 Phototransistors, Yin, Zongyou & Li, Hai & Li, (Colin) Hong & Jiang, Lin & Shi, Yumeng & Sun, Yinghui & Lu, Gang & Zhang, Qing & Chen, Xiaodong & Zhang, Hua, https://doi.org/10.1021/nn2024557
Ti/Au electrodes
SiO2 (300 nm)
Si (bottom gate)
MoS2 layer
MoS2 layer:
Channel length L = 2.1 um
Channel width W = 2.6 um
Channel thickness th = 0.8 nm
Main parameters:
mu = 0.11 cm2/(V*s)
ON/OFF ∝ 103
Deposition method – mechanical exfoliation

## Slide 52: Comparison with the data from literature:
3) Radisavljevic, B., Radenovic, A., Brivio, J. et al. Single-layer MoS2 transistors. Nature Nanotech 6, 147–150 (2011). https://doi.org/10.1038/nnano.2010.279
Main parameters:
mu (for back gate) ∝ 217 cm2/(V*s)
MoS2 layer:
Channel width W = 4 um
Channel length L = 1.5 um
Channel thickness th = 0.65 nm
Channel-Back gate capacitance per unit area: Ci = 1.3*10-4 F/m2
The result is not truly concrete, since in the same paragraph
they mention the mobility of 0.1-10 cm2/(V*s).
Deposition method – mechanical exfoliation