## Slide 1: Report 22/11/2023
X-Ray measurements on the samples from Batch 2

## Slide 2
Batch | Sample | device | ON/OFF | SS (V/dec) | Vth (V) | mu (cm^2/(V*s) | Sensitivity | Comments
2 | 1 | 1 |  |  |  |  |  | 
 |  | 2 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 |  | 4 |  |  |  |  |  | 
 |  | 5 |  |  |  |  |  | 
 | 4 | 1 |  |  |  |  |  | 
 | 5 | 1 |  |  |  |  |  | 
 |  | 2 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 |  | 4 |  |  |  |  |  | 
 | 6 | 1 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 |  | 5 |  |  |  |  |  | 
 | 7 | 1 |  |  |  |  |  | 
 |  | 4 |  |  |  |  |  | 
 |  | 5 |  |  |  |  |  | 
 | 8 | 1 |  |  |  |  |  | 
 | 9 | 2 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 | 10 | 1 |  |  |  |  |  | 
 |  | 2 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 |  | 5 |  |  |  |  |  | 
 |  | 6 |  |  |  |  |  | 
 | 11 | 1 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 | 12 | 1 |  |  |  |  |  | 
 |  | 2 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 |  | 4 |  |  |  |  |  | 
 | 14 | 1 |  |  |  |  |  | 
 |  | 2 |  |  |  |  |  | 
 |  | 3 |  |  |  |  |  | 
 |  | 4 |  |  |  |  |  | 

## Slide 3: Calibration Plot (distance 32 cm from the chassis)

## Slide 4: Sample1_device1
th=4.5±0.5 nm
W = …

## Slide 5: Sample1_device1

## Slide 6: Sample1_device3
th=6.0±0.6 nm

## Slide 7: Sample1_device3

## Slide 8: Sample1_device3

## Slide 9: Sample1_device3

## Slide 10: Sample1_device3

## Slide 11: Sample4_device1

## Slide 12: Sample4_device1
NO CURRENT -> SEEMS THAT AU ELECTRODES
DEGRADED

## Slide 13: Sample6_device1

## Slide 14: Sample6_device1

## Slide 15: Sample6_device1

## Slide 16: Sample6_device1

## Slide 17: Sample6_device1

## Slide 18: Sample6_device5

## Slide 19: Sample6_device5

## Slide 20: Sample7_device1

## Slide 21: Sample7_device1

## Slide 22: Sample8_device1

## Slide 23: Sample8_device1

## Slide 24: Sample9_device3

## Slide 25: Sample9_device3
SHORT CIRCUIT BETWEEN GATE AND DRAIN/SOURCE

## Slide 26: Sample10_device3

## Slide 27: Sample10_device3
NO CURRENT
(VERIFIED ALSO IN HORIZONTAL POSITION)

## Slide 28: Sample10_device6

## Slide 29: Sample10_device6
SHORT CIRCUIT

## Slide 30: Sample11_device3

## Slide 31: Sample11_device3
NO SENSE

## Slide 32: Sample12_device2

## Slide 33: Sample12_device2
DRAIN CURRENT REACHES MIRCOAMPS ONLY AT
50 V, WHICH IS TOO LOW
FOR REACHING PHOTOCONDUCTIVE GAIN

## Slide 34: Sample12_device3

## Slide 35: Sample12_device3

## Slide 36: Sample12_device3

## Slide 37: Sample12_device4

## Slide 38: Sample12_device4

## Slide 39: Sample12_device4

## Slide 40: Sample14_device1

## Slide 41: Sample14_device1

## Slide 42: Sample14_device1

## Slide 43: Sample14_device2

## Slide 44: Sample14_device2

## Slide 45: Sample14_device2

## Slide 46: Sample14_device3

## Slide 47: Sample14_device3
At 40 V peaks are very small already at 500 uA,
so I stopped here and increased VGate to 50 V

## Slide 48: Sample14_device3

## Slide 49: Sample14_device4 (15/11)

## Slide 50: Sample14_device4 (15/11)

## Slide 51: Sample14_device4 (15/11)

## Slide 52: Sample14_device4 (15/11)

## Slide 53: Sample14_device4 (22/11)

## Slide 54: Sample14_device4 (22/11)

## Slide 55: Sample14_device4 (22/11)