## Slide 1: Report batch 20230412_Parylene

## Slide 2: General features
Batch made up of 8 substrates, each one of them containing 4 OFETs with common gate
The first 4 substrates are coated by Parylene-C, an electrically insulating polymer
TMTES:PS as active material, with fixed 2:1 ratio and 280K molecular weight
Channel features: L=25µm, W=2500µm, C=17.3·F/

## Slide 3: Parylene samples: working devices

## Slide 4: X-rays measurements: Current normalization
Polynomial fit before irradiation

## Slide 5: X-rays measurements: sensitivity calculation
After the normalization, the photocurrent is calculated as ( indicated before as green and red dots, respectively)
For every dose rate, 3 photocurrent values are calculated and averaged (given their compatibility)
The plot of the photocurrents vs dose rate provides the sensitivity of the device, defined as the slope of the linear fit

## Slide 6: Parylene samples

## Slide 7: Parylene samples
Transfer characteristics
Output characteristic (example)
:Working point ()

## Slide 8: Parylene: Current curves

## Slide 9: Parylene: Photocurrent

## Slide 10: Parylene: Transfer characteristic

## Slide 11: Parylene: Transfer before and after X-rays
Quantity |  | 
Value before X-rays | 2.5±0.5 | 1.0±0.1
Value after X-rays | 2.4±0.3 | 1.8±0.2
Percentage variation | -3% | +85%
Quantity |  | 
Value before X-rays | 2.5±0.5 | 1.0±0.1
Value after X-rays | 2.4±0.3 | 1.8±0.2
Percentage variation | -3% | +85%

## Slide 12: Summary table: Parylene
OFET | Characterization | µ () |  | SS (V/decade) | Sensitivity (·)
S1_OFET1 | Electrical, X-rays | 2.58±0.08 | 1.94±0.06 | 2.07±0.06 | 14±1
S1_OFET2 | Electrical | 2.37±0.07 | 2.04±0.06 | 2.03±0.06 | No
S2_OFET1 | Electrical, X-rays | 2.67±0.08 | 1.78±0.05 | 1.80±0.05 | 14.7±0.6
S2_OFET2 | Electrical | 2.46±0.07 | 1.54±0.05 | 1.57±0.05 | No
S2_OFET3 | Electrical | 2.54±0.08 | 1.36±0.04 | 1.57±0.05 | No
S2_OFET4 | Electrical | 2.39±0.07 | 1.18±0.04 | 1.29±0.04 | No
S3_OFET1 | Electrical, X-rays | 2.34±0.07 | 1.78±0.05 | 1.80±0.05 | 16.3±0.4
S3_OFET2 | Electrical | 2.40±0.07 | 1.93±0.06 | 1.92±0.06 | No
S4_OFET1 | Electrical, X-rays | 1.88±0.05 | 1.81±0.05 | 1.77±0.05 | 9.9±0.3
S4_OFET2 | Electrical | 1.74±0.08 | 1.63±0.05 | 1.59±0.05 | No
OFET | Characterization |  |  | SS (V/decade) | 
S1_OFET1 | Electrical, X-rays | 2.58±0.08 | 1.94±0.06 | 2.07±0.06 | 14±1
S1_OFET2 | Electrical | 2.37±0.07 | 2.04±0.06 | 2.03±0.06 | No
S2_OFET1 | Electrical, X-rays | 2.67±0.08 | 1.78±0.05 | 1.80±0.05 | 14.7±0.6
S2_OFET2 | Electrical | 2.46±0.07 | 1.54±0.05 | 1.57±0.05 | No
S2_OFET3 | Electrical | 2.54±0.08 | 1.36±0.04 | 1.57±0.05 | No
S2_OFET4 | Electrical | 2.39±0.07 | 1.18±0.04 | 1.29±0.04 | No
S3_OFET1 | Electrical, X-rays | 2.34±0.07 | 1.78±0.05 | 1.80±0.05 | 16.3±0.4
S3_OFET2 | Electrical | 2.40±0.07 | 1.93±0.06 | 1.92±0.06 | No
S4_OFET1 | Electrical, X-rays | 1.88±0.05 | 1.81±0.05 | 1.77±0.05 | 9.9±0.3
S4_OFET2 | Electrical | 1.74±0.08 | 1.63±0.05 | 1.59±0.05 | No
,

## Slide 13: No parylene samples (common features)

## Slide 14: No parylene samples
Transfer characteristics*
Output characteristic (example)
:Working point ()
*OFET3 and 4 of every sample are not shown to improve clarity

## Slide 15: No parylene: Transfer characteristic

## Slide 16: Summary table: No parylene
OFET | Characterization | µ () |  | SS (V/decade) | Sensitivity ()
S5_OFET1 | Electrical, X-rays | 2.71±0.08 | 1.46±0.04 | 1.21±0.04 | (11.0±0.6)·
S5_OFET2 | Electrical, X-rays | 3.16±0.09 | 1.28±0.04 | 0.99±0.03 | (11.0±1)·
S5_OFET3 | Electrical | 2.70±0.08 | 0.73±0.02 | 0.45±0.01 | No
S5_OFET4 | Electrical | 2.66±0.08 | 0.79±0.02 | 0.49±0.01 | No
S6_OFET1 | Electrical, X-rays | 2.54±0.08 | 0.96±0.03 | 0.60±0.02 | (2.4±0.3)·
S6_OFET2 | Electrical | 2.22±0.08 | 1.26±0.04 | 0.94±0.03 | No
S6_OFET3 | Electrical | 2.52±0.07 | 0.86±0.03 | 0.50±0.02 | No
S6_OFET4 | Electrical | 2.46±0.08 | 0.93±0.03 | 0.54±0.02 | No
S7_OFET1 | Electrical, X-rays | 2.34±0.07 | 0.80±0.02 | 0.56±0.02 | Meaningless
S7_OFET2 | Electrical, X-rays | 2.39±0.07 | 1.04±0.03 | 0.79±0.02 | -(6±2)·
S7_OFET3 | Electrical | 2.04±0.06 | 1.29±0.04 | 0.99±0.03 | No
S7_OFET4 | Electrical, X-rays | 2.38±0.07 | 1.29±0.04 | 0.99±0.03 | Meaningless
S8_OFET1 | Electrical, X-rays | 2.69±0.08 | 0.89±0.03 | 0.44±0.01 | (1.6±0.1)·
S8_OFET2 | Electrical, X-rays | 2.83±0.08 | 1.21±0.04 | 0.89±0.03 | Meaningless
S8_OFET3 | Electrical | 2.91±0.09 | 0.92±0.03 | 0.55±0.02 | No
S8_OFET4 | Electrical, X-rays | 2.62±0.08 | 2.40±0.07 | 2.34±0.07 | (8±2)·
OFET | Characterization |  |  | SS (V/decade) | 
S5_OFET1 | Electrical, X-rays | 2.71±0.08 | 1.46±0.04 | 1.21±0.04 | 
S5_OFET2 | Electrical, X-rays | 3.16±0.09 | 1.28±0.04 | 0.99±0.03 | 
S5_OFET3 | Electrical | 2.70±0.08 | 0.73±0.02 | 0.45±0.01 | No
S5_OFET4 | Electrical | 2.66±0.08 | 0.79±0.02 | 0.49±0.01 | No
S6_OFET1 | Electrical, X-rays | 2.54±0.08 | 0.96±0.03 | 0.60±0.02 | 
S6_OFET2 | Electrical | 2.22±0.08 | 1.26±0.04 | 0.94±0.03 | No
S6_OFET3 | Electrical | 2.52±0.07 | 0.86±0.03 | 0.50±0.02 | No
S6_OFET4 | Electrical | 2.46±0.08 | 0.93±0.03 | 0.54±0.02 | No
S7_OFET1 | Electrical, X-rays | 2.34±0.07 | 0.80±0.02 | 0.56±0.02 | Meaningless
S7_OFET2 | Electrical, X-rays | 2.39±0.07 | 1.04±0.03 | 0.79±0.02 | 
S7_OFET3 | Electrical | 2.04±0.06 | 1.29±0.04 | 0.99±0.03 | No
S7_OFET4 | Electrical, X-rays | 2.38±0.07 | 1.29±0.04 | 0.99±0.03 | Meaningless
S8_OFET1 | Electrical, X-rays | 2.69±0.08 | 0.89±0.03 | 0.44±0.01 | 
S8_OFET2 | Electrical, X-rays | 2.83±0.08 | 1.21±0.04 | 0.89±0.03 | Meaningless
S8_OFET3 | Electrical | 2.91±0.09 | 0.92±0.03 | 0.55±0.02 | No
S8_OFET4 | Electrical, X-rays | 2.62±0.08 | 2.40±0.07 | 2.34±0.07 | 

## Slide 17: Sample5: Current curves

## Slide 18: Sample5: Photocurrent

## Slide 19: Sample5: Transfer before and after X-rays
Quantity |  | 
Value before X-rays | 2.88±0.09 | 0.68±0.02
Value after X-rays | 2.93±0.09 | 1.06±0.03
Percentage variation | +2% | +56%
Quantity |  | 
Value before X-rays | 2.88±0.09 | 0.68±0.02
Value after X-rays | 2.93±0.09 | 1.06±0.03
Percentage variation | +2% | +56%

## Slide 20: Sample6: Current curves

## Slide 21: Sample6: Photocurrent

## Slide 22: Sample6: Transfer before and after X-rays
Quantity |  | 
Value before X-rays | 2.16±0.06 | 0.14±0.01
Value after X-rays | 2.22±0.06 | 0.41±0.01
Percentage variation | +3% | +192%
Quantity |  | 
Value before X-rays | 2.16±0.06 | 0.14±0.01
Value after X-rays | 2.22±0.06 | 0.41±0.01
Percentage variation | +3% | +192%

## Slide 23: Sample7: Current curves

## Slide 24: Sample7: Photocurrent

## Slide 25: Sample7: Transfer before and after X-rays
Quantity |  | 
Value before X-rays | 2.13±0.06 | 0.88±0.02
Value after X-rays | 2.03±0.06 | 0.89±0.02
Percentage variation | -5% | +1%
Quantity |  | 
Value before X-rays | 2.13±0.06 | 0.88±0.02
Value after X-rays | 2.03±0.06 | 0.89±0.02
Percentage variation | -5% | +1%

## Slide 26: Sample8: Current curves

## Slide 27: Sample8: Photocurrent

## Slide 28: Sample8: Transfer before and after X-rays
100K |  | 
Value before X-rays | 2.05±0.06 | 1.94±0.06
Value after X-rays | 2.12±0.06 | 1.78±0.06
Percentage variation | +3% | -8%
100K |  | 
Value before X-rays | 2.05±0.06 | 1.94±0.06
Value after X-rays | 2.12±0.06 | 1.78±0.06
Percentage variation | +3% | -8%

## Slide 29: Composition comparisons

## Slide 30: Transfer characteristic
The leakage current is remarkably high in samples coated with parylene
Parylene samples have a slightly worse shape of the transfer characteristic
Parylene samples electrical parameters have less fluctuations (see next slides)

## Slide 31: Electric parameters: SS and

## Slide 32: Electric parameters: Mobility

## Slide 33
Electric parameters:
Composition | () |  | SS (V/decade)
Parylene | 2.3±0.3 | 1.7±0.3 | 1.7±0.2
No parylene | 2.6±0.3 | 1.1±0.4 | 0.7±0.5
Sample5 | 2.8±0.2 | 1.1±0.4 | 0.8±0.4
Sample6 | 2.4±0.1 | 1.0±0.2 | 0.6±0.2
Sample7 | 2.3±0.2 | 1.1±0.2 | 0.8±0.2
Sample8 | 2.8±0.1 | 1.4±0.7 | 1.1±0.9
Composition |  |  | SS (V/decade)
Parylene | 2.3±0.3 | 1.7±0.3 | 1.7±0.2
No parylene | 2.6±0.3 | 1.1±0.4 | 0.7±0.5
Sample5 | 2.8±0.2 | 1.1±0.4 | 0.8±0.4
Sample6 | 2.4±0.1 | 1.0±0.2 | 0.6±0.2
Sample7 | 2.3±0.2 | 1.1±0.2 | 0.8±0.2
Sample8 | 2.8±0.1 | 1.4±0.7 | 1.1±0.9
Parylene samples have worse electrical parameters
On the other hand, their electrical parameters have smaller standard deviations

## Slide 34
X-rays detection: currents in time

## Slide 35
X-rays detection: currents in time
Parylene samples and Sample5 have similar current trends
Sample6 and Sample7 have an initial current drop, followed by a recover
Sample8 is different from all the others, and is quite similar to batch0315
This last sample is the only one following the behaviour that we would expect, since sample without parylene are identical (in composition) to batch0315

## Slide 36
X-rays detection: normalized currents

## Slide 37
X-rays detection: normalized currents
Parylene samples and Sample5 have similar photocurrent trends, with a triangular shape and a very good homogeneity
Sample6 photocurrent is influenced by the initial current drop
Sample7 photocurrents are always negative
Sample8 photocurrent is different from all the others, but is quite different from the batch0315 ones, due to the presence of smooth peaks

## Slide 38: Sensitivity comparison

## Slide 39: Resume on electical parameters variation after X-rays irradiation
Composition |  | 
No parylene | +2% | +121%
Parylene | -3% | +85%
Sample5 | +2% | +56%
Sample6 | +3% | +192%
Sample7 | -5% | +1%
Sample8 | +3% | -8%
Composition |  | 
No parylene | +2% | +121%
Parylene | -3% | +85%
Sample5 | +2% | +56%
Sample6 | +3% | +192%
Sample7 | -5% | +1%
Sample8 | +3% | -8%
Mobilities tend to remain stable after irradiation in all samples
Samples without parylene have no common behaviour when it comes to threshold voltage
Sample5 and Sample6 have important increases in the threshold voltage, while Sample7 and Sample8 retain their transfer curves after the irradiation

## Slide 40: Conclusions
Samples with parylene show a «triangle-like» photocurrent that is present with very small deviations in all the samples
Sample5 is very similar to parylene samples under every aspect, although no clear reason for this has been found
Samples without parylene appear to be very different from each other
Even if the composition is the same of batch0315, they look very different in current shapes (Sample8 is the more similar to batch0315)
Sample7 show negative photocurrents