## Slide 1: Batch 20230315/Batch 20230427/Batch20230508 impact of PS Molecular Weight and Ratio
UNIBO May 2023
AIM of these measurements  see if the different PS molecular weight and the different ratio TMTES:PS have an impact on the X-Ray detection performances

## Slide 2: Impact of different TMTES:PS RATIO
The only trend with ratio is for 280K  the sensitivity decreases with the increasing of PS concentration.
WHY?
  Is the TOF SIMS different for the three MW? Is the segregation of PS different?
  The mobility also tends to decrease with the PS concentration. Could this aspect be the main reason of the sensitivity trend?
We couldn’t determine the sensitivity of the 1:2 ratio and 10K and 100K MW because the X-rays provoked a decrease in the current signal instead of an increase…
  Can we see any difference with the TOF-SIMS?
VGS = -2.5 V; VDS = -10 V
(Biases are DIFFERENT from those used in previously published works)
4:1 | 2:1 | 1:2
µ = (2.3±0.3) cm2 V-1 s-1 | µ = (0.8±0.3) cm2 V-1 s-1 | µ = (0.9±0.4) cm2 V-1 s-1

## Slide 3: Impact of different PS Molecular Weigth
We can confirm what we saw in the first batch (ratio 2:1)  it seems that the different MW hasn’t a strong impact (or not clear) on the X-Ray sensitivity.
 In this case it seems to follow the mobility
VGS = -2.5 V; VDS = -10 V
(Biases are DIFFERENT from those used in previously published works)

## Slide 4: Comparison with TIPS:PS @ different Ratio
TIPS:PS |  | 
Ratio | Mobility (cm2 V-1 s-1) | Sensitivity (uC Gy-1 cm-2)
4:1 | 0.5±0.2 | 13 × 103
2:1 | 0.5±0.3 | 13 × 103
1:1 | 0.06±0.04 | 0.5 × 103
TMTES:PS |  | 
Ratio | Mobility (cm2 V-1 s-1) | Sensitivity (uC Gy-1 cm-2)
4:1 | 1.4±0.4 | (44±3) × 103
2:1 | 0.8±0.2 | (37±14) × 103
1:2 | 0.8±0.1 | (18±3) × 103
Different trend but variations of the same order of magnitude
VGS = -15 V; VDS = -20 V
(SAME conditions used in previous works)

## Slide 5: SoA comparison
If we compare the TMTES:PS 2:1 280K characterized in the same polarization conditions, the mobilities of the new samples are lower than in the past and the sensitivity is lower as well due to the ‘worse’ transport properties.  we are consistent with the data reported in the last work!
The anomalous effect under irradiation (e.g. discharge) occoured only with the 1:2 ratio. The TOF SIMS is different for these samples? The increase of PS makes some difference on the segregation of PS?

## Slide 6: Conclusions
IMPACT OF DIFFERENT TMTES:PS RATIOS  The only trend with ratio is for 280K. The sensitivity decreases with the increasing of PS concentration
IMPACT OF DIFFERENT PS MOLECULAR WEIGHT  It seems that the different MWs doesn’t seem to have a strong impact on the X-Ray sensitivity
DETECTION PERFORMANCE DEPENDENCE ON PS Sensitivity decreases with PS concentration and lower MW. Comparison with TOF-SIMS is needed to fully understand these data
COMPARISON WITH SoA: Lower mobility  lower sensitivity