## Slide 1: Samples structure and characterization
MEASUREMENTS
n-type semiconductor
Low stability in aire, storage in glove box
Electrical measurements were performed reaching VDS = 1 V, and VGS = -60 to 60 V
Delay 100 ms and ΔVGS = 0.5 V
Top contact / Bottom gate
Note: If you need, you can scratch the surface of the substrates to access the gate.
Au/Cr 45/3 nm
MoS2
BCB layer 50 nm
SiOx 278 nm
Si

## Slide 2
Sample 1
Device 1
Device 2
Device 3
Device 4
Device 5
Thickness
Device 1 = 4.5±0.5 nm
Device 2 = 5.4±0.7 nm
Device 3 = 6.0±0.6 nm
Device 4 = 2.6±0.3 nm
Device 5 = 2.9±0.7 nm
Device 1
Device 2
Device 3
Device 4
Device 5

## Slide 3
Sample 1
Device 1
Device 2
Device 3
Device 4
Device 5
Thickness
Device 1 = 4.5±0.5 nm
Device 2 = 5.4±0.7 nm
Device 3 = 6.0±0.6 nm
Device 4 = 2.6±0.3 nm
Device 5 = 2.9±0.7 nm
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 4
Sample 4
Thickness
Device 1 = 2.4±0.3 nm
Device 2 = -
Device 3 = -
Device 4 = -
Device 1
Device 2
Device 3
Device 4
Device 1
Device 2
Device 3
Device 4

## Slide 5
Sample 4
Thickness
Device 1 = 2.4±0.3 nm
Device 2 = -
Device 3 = -
Device 4 = -
Device 1
Device 2
Device 3
Device 4

## Slide 6
Sample 5
Thickness
Device 1 = 8.9±0.9 nm
Device 2 = 5.8±0.9 nm
Device 3 = 2.8±0.4 nm
Device 4 = 3.1±0.5 nm
Device 1
Device 3
Device 2
Device 4
Device 1
Device 2
Device 3
Device 4

## Slide 7
Sample 5
Thickness
Device 1 = 8.9±0.9 nm
Device 2 = 5.8±0.9 nm
Device 3 = 2.8±0.4 nm
Device 4 = 3.1±0.5 nm
Device 1
Device 2
Device 3
Device 4
Device 1
Device 2
Device 4
Device 3

## Slide 8
Sample 6
Thickness
Device 1 = 8.3±0.9 nm
Device 2 = -
Device 3 = 10.8±0.6 nm
Device 4 = -
Device 5 = 6.3±0.6 nm
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 9
Sample 6
Device 3
Device 1
Device 5
Thickness
Device 1 = 8.3±0.9 nm
Device 2 = -
Device 3 = 10.8±0.6 nm
Device 4 = -
Device 5 = 6.3±0.6 nm
Device 1
Device 2
Device 3
Device 4
Device 5

## Slide 10
Sample 7
Thickness
Device 1 = 2.8±0.4 nm
Device 2 = -
Device 3 = -
Device 4 = 3.8±0.4 nm
Device 5 = 5.7±0.3 nm
Device 1
Device 3
Device 5
Device 2
Device 4
Device 1
Device 2
Device 3
Device 4
Device 5

## Slide 11
Sample 7
Device 1
Device 5
Device 4
Thickness
Device 1 = 2.8±0.4 nm
Device 2 = -
Device 3 = -
Device 4 = 3.8±0.4 nm
Device 5 = 5.7±0.3 nm
Device 1
Device 2
Device 3
Device 4
Device 5

## Slide 12
Sample 8
Thickness
Device 1 = 6.2±0.6 nm
Device 2 = -
Device 3 = -
Device 4 = -
Device 5 = -
Device 1
Device 2
Device 3
Device 4
Device 5
Device 6
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 13
Sample 8
Thickness
Device 1 = 2.8±0.4 nm
Device 2 = -
Device 3 = -
Device 4 = 3.8±0.4 nm
Device 5 = 5.7±0.3 nm
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1

## Slide 14
Sample 9
Thickness
Device 1 = -
Device 2 = 7.8±0.7 nm
Device 3 = 10.8±1.4 nm
Device 1
Device 2
Device 3
Device 1
Device 2
Device 3

## Slide 15
Sample 9
Thickness
Device 1 = -
Device 2 = 7.8±0.7 nm
Device 3 = 10.8±1.4 nm
Device 1
Device 2
Device 3
Device 2
Device 3

## Slide 16
Sample 10
Thickness
Device 1 = 3.9±0.5 nm
Device 2 = 2.6±0.3 nm
Device 3 = 8.7±0.4 nm
Device 4 = -
Device 5 = 8.0±0.5 nm
Device 6 = 9.4±0.5 nm
Device 1
Device 3
Device 2
Device 4
Device 5
Device 6
Device 1
Device 2
Device 3
Device 4
Device 5
Device 6

## Slide 17
Sample 10
Thickness
Device 1 = 3.9±0.5 nm
Device 2 = 2.6±0.3 nm
Device 3 = 8.7±0.4 nm
Device 4 = -
Device 5 = 8.0±0.5 nm
Device 6 = 9.4±0.5 nm
Device 1
Device 2
Device 3
Device 4
Device 5
Device 6
Device 1
Device 3
Device 6
Device 2
Device 5

## Slide 18
Sample 11
Thickness
Device 1 = 3.6±0.4 nm
Device 2 = -
Device 3 = 9.2±0.8 nm
Device 4 = -
Device 5 = -
Device 2
Device 4
Device 1
Device 3
Device 5
Device 1
Device 2
Device 3
Device 4
Device 5

## Slide 19
Sample 11
Thickness
Device 1 = 3.6±0.4 nm
Device 2 = -
Device 3 = 9.2±0.8 nm
Device 4 = -
Device 5 = -
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1
Device 3

## Slide 20
Sample 12
Thickness
Device 1 = 4.8±0.6 nm
Device 2 = 2.4±0.3 nm
Device 3 = 3.3±0.3 nm
Device 4 = 4.8±0.3 nm
Device 5 = -
Device 1
Device 2
Device 3
Device 4
Device 5
Device 1
Device 3
Device 5
Device 2
Device 4

## Slide 21
Sample 12
Thickness
Device 1 = 4.8±0.6 nm
Device 2 = 2.4±0.3 nm
Device 3 = 3.3±0.3 nm
Device 4 = 4.8±0.3 nm
Device 5 = -
Device 1
Device 2
Device 3
Device 4
Device 5
Device 3
Device 4
Device 1
Device 2

## Slide 22
Sample 14
Thickness
Device 1 = 4.8±0.6 nm
Device 2 = 2.4±0.3 nm
Device 3 = 3.3±0.3 nm
Device 4 = 4.8±0.3 nm
Device 2
Device 4
Device 1
Device 3
Device 1
Device 2
Device 3
Device 4

## Slide 23
Sample 14
Device 4
Device 2
Device 3
Device 1
Thickness
Device 1 = 4.8±0.6 nm
Device 2 = 2.4±0.3 nm
Device 3 = 3.3±0.3 nm
Device 4 = 4.8±0.3 nm
Device 1
Device 2
Device 3
Device 4

## Slide 24: Blank devices
List:
  Sample 6 Device 2
  Sample 10 Device 4
  Sample 11 Device 2
  Sample 11 Device 4